| Name | Softell |
| --- | --- |
| Grade | TBP 237D NAT |
| Resin type | Advanced Polyolefin |
| Description | Softell TBP 237D Nat is a high performance thermoplastic polyolefin, designed for use in applications where softness and elasticity is a key requirement. This product is in an experimental phase. |
| Availability | Europe, North America, Asia-Pacific, Australia-NZ, Africa-Middle East, South & Central America |

| Technical data |  |
| --- | --- |
| Tensile Strength @ Break | 10.0 MPa |
| Tensile Elongation @ Brk | 800 % (Injection Molded) |
| Melt flow rate (MFR) | 0.60 g/10 min (230°C/2.16Kg) |