| Name | Softell |
| --- | --- |
| Grade | Q 020 F |
| Resin type | Advanced Polyolefin |
| Description | Softell Q 020 F is a high performance thermoplastic polyolefin designed for use in applications where softness and elasticity is a key requirement. It features a level of flexibility, toughness and softness that is comparable with many other plastomers and elastomers. Thanks to its unique morphology however, it retains some typical polyolefin characteristics like the processability, a high thermal stability and an excellent compatibility with other polyolefins. The product can be easily processed on conventional LDPE or LLDPE blown film lines. Combining Softell Q 020 F with conventional PP and PE allows a very wide range of blown film types to be produced as blends and/or multilayer structures Softell Q 020 F does not contain any slip or anti-blocking agents. This grade is available in natural pellets. For Regulatory information, please refer to this product's RAPIDS, which can be found on www.basell.com. |
| Availability | Europe, North America, Asia-Pacific, Australia-NZ, Africa-Middle East, South & Central America |

| Technical data |  |
| --- | --- |
| Tensile Strength @ Break | 10.0 MPa |
| Tensile Elongation @ Brk | 800 % (Injection Molded) |
| Density | 0.870 g/cm³ (Method A) |
| Melt flow rate (MFR) | 0.60 g/10 min (230°C/2.16Kg) |
| Flexural modulus | 20.0 MPa |
| Notched izod impact strength | No Break kJ/m² (-50 °C) |
| Vicat softening temperature | 41.0 °C (A50 (50°C/h 10N)) |
| Shore hardness | 75 (Shore A) |