| Name | Softell |
| --- | --- |
| Grade | CA 02 A |
| Resin type | Advanced Polyolefin |
| Description | Softell CA 02 A is a thermoplastic polyolefin made by Basell`s proprietary Catalloy technology. It has been developed for the extrusion, calendering and extrusion blow moulding of very soft film and sheet. Thanks to its high rubber content Softell CA 02 A features outstanding low stiffness, excellent low hardness and very good impact resistance. Softell CA 02 A shows high compatibility to fillers and flame retardent agencies as well as to other polyolefins. The grade is available in natural pellet form. Further informations can be provide on request. |
| Availability | Europe, North America, Asia-Pacific, Australia-NZ, Africa-Middle East, South & Central America |

| Technical data |  |
| --- | --- |
| Flame rating - UL | HB (1.50 mm) |
| Flame rating - UL | HB (3.00 mm) |
| Relative temperature index Mech w/oImp | 50 °C (1.50 mm) |
| Relative temperature index Mech w/oImp | 50 °C (3.00 mm) |
| Relative temperature index Mech w/Imp | 50 °C (1.50 mm) |
| Relative temperature index Mech w/Imp | 50 °C (3.00 mm) |
| Relative temperature index | 50 °C (1.50 mm) |
| Relative temperature index | 50 °C (3.00 mm) |
| Density | 0.870 g/cm³ (Method A) |
| Melt flow rate (MFR) | 0.6 g/10 min (230°C/2.16Kg) |
| Tensile Stress at Break | 10 MPa (23 °C) |
| Tensile Stress at Yield | 10 MPa (23 °C °C) |
| Tensile Strain at Break | >500 % (23 °C °C) |
| Flexural modulus | 20 MPa |
| Vicat softening temperature | 41 °C (A50 (50°C/h 10N)) |
| Shore hardness | 75 (Shore A) |